## Slide 1: Kokam 75 Ah NMC-Gr Aging For Sunpower (2015-2017)
Published in ACC 2017 proceedings
10.23919/ACC.2017.7963578

## Slide 2: Test matrix
Testing protocol
All cells at beginning of life
  5x C/5 cycles
  HPPC
  RPT: 1x C/5 cycle, HPPC
Calendar aging cells: charge to SOC, rest at open-circuit
Cycle aging cells: CCCV cycling with rests
RPTs every 3 weeks
HPPC
5x C/5
RPT
Cycling

## Slide 3: Cell_01 – Cycling: 23 °C, 80% DOD, 92% SOCmax (replicate with cell_02)

## Slide 4: Cell_02 – Cycling: 23 °C, 80% DOD, 92% SOCmax (replicate with cell_01)

## Slide 5: Cell_03 – Cycling: 30 °C, 100% DOD

## Slide 6: Cell_04 – Cycling: 30 °C, 80% DOD, 92% SOCmax (50% duty cycle)

## Slide 7: Cell_05 – Calendar: 30 °C, 100% SOC

## Slide 8: Cell_06 – Cycling: 0 °C, 80% DOD, 92% SOCmax (replicate with cell_07)

## Slide 9: Cell_07 – Cycling: 0 °C, 80% DOD, 92% SOCmax (replicate with cell_06)

## Slide 10: Cell_08 – Calendar: 45 °C, 65% SOC

## Slide 11: Cell_09 – Cycling: 45 °C, 80% DOD, 92% SOCmax

## Slide 12: Cell_10 – Calendar: 45 °C, 100% SOC

## Slide 13: Cell_11 – Calendar: 55 °C, 100% SOC (RPT @ 45 °C)